Tel: (4725) 46 95 65

Requirements for aluminum scrap according to GOST R 54564-2011

- Scrap and lump waste of aluminum should not be clogged with other metals and alloys, oil paints, resin, oil products, construction waste, polymeric materials, moisture, ice, snow.

- The aluminum content in the scrap should be at least 96%.

- The sizes of the pieces should be no more than 1500*1500*1000 mm, the profile should not exceed a length of 1500 mm.

- Sizes of packages should be no more than 500*500*700 mm.

- Cable scrap must be freed from insulation, packed in bundles, coils, piles or packages.

- Scrap and lump waste of aluminum should not have radioactivity.

- Scrap and lump waste of aluminum should not contain explosive objects.

- The degree of pollution of scrap and lumpy waste of aluminum with harmful substances should not exceed the MPC established by GOST 12.1.005, GOST 12.1.007, GOST 2874.

- Scrap and lump waste of aluminum should be of the following grades: A999, A99, A995, A97, A95, A85, A8, A5, A5E, A0, ADoch, ADch, AD000, AD00, AD0, AD0E, AD1, AD31, AA6063, AA6060.

- Vehicles for transportation of scrap should provide side unloading, with a body length of more than 3.2 m and the top, if the scrap is in the "Big Bag". Rear unloading of bulky scrap is not permissible.

- Metal should be sorted into groups: AD; food; electrotechnical, when re-grading, additional costs for unloading are borne by scrap suppliers.

Best regards,

General Director of ALTEK LLC                                  E.G. Shcherbina